WEST VIRGINIA DEPARTMENT OF TRANSPORTATION

DIVISION OF HIGHWAYS

MATERIALS CONTROL, SOILS AND TESTING DIVISION

MATERIALS PROCEDURE

GUIDE FOR QUALITY CONTROL PLANS

FOR ASPHALT CONCRETE

# PURPOSE

## This procedure presents uniform Quality Control guidelines which should be used when the Contractor (Producer) develops their Quality Control Plan.  All items listed are believed necessary to assure adequate product Quality Control.

## This procedure also creates a more uniform process for District Materials to review and approve Quality Control Plans for use on projects.

# SCOPE

## This procedure is applicable to asphalt concrete base, wearing, and patching-and- leveling courses.

# GENERAL REQUIREMENTS

## As stated in the specifications, a Quality Control Plan must be developed by the producer and submitted to the Engineer prior to construction. Acceptance of the Quality Control Plan by the Engineer will be contingent upon its concurrence with these guidelines. For this reason, the plan should clearly describe the methods by which the Quality Control Program will be conducted. For example, the items to be controlled, tests to be performed, testing frequencies, sampling locations and techniques all should be included and each item should be listed separately. Also, a detailed plan of action regarding disposition of non-specification material should be included.  Such a plan should provide for immediate notification of all parties involved in the event non-conforming situations are detected. Attachment 1 may be used as an example Quality Control Plan for plant operations using all items that are applicable to the specific type of plant items produced. Attachment 2 may be used as an example Quality Control Plan for field operations using all items that are applicable to field work.

## Inspection and testing records should shall be maintained, kept current, and made available for review by the Engineer throughout the life of the contract. All other documentation, such as date of inspections, tests performed, temperature measurements, and any accuracy, calibration, or re-calibration checks performed on production or testing equipment should be recorded.

## The Contractor should shall maintain standard calibrated equipment and qualified personnel in accordance with contract and specification requirements for the item(s) being produced.

# QUALITY CONTROL PLAN

## The Contractor must submit the Field Quality Control Plan yearly to each District in which their projects are located.  The Contractor must also submit the Plant Quality Control Plan yearly to the District in which the plant is located. Any modification to these plans for special conditions on a specific project will require the submittal of an addendum to the Quality Control Plan which shall include all approved changes specific to that project. Distribution of the approved Quality Control Plan will be made by the Division.

## The Yearly Master Field Quality Control Plan shall be for the duration of one calendar year beginning on January 1st and ending on December 31st.

## The District will review the submitted Master Quality Control Plan and assign a laboratory reference number upon approval.  The District will acknowledge approval of Yearly Quality Control Plan to the Contractor by letter, which will include the laboratory reference number and a copy of the approved Yearly Master Quality Control Plan.   This will then be scanned and placed in ProjectWise under the appropriate District’s Org for that Contractor.

### The laboratory reference number for a Yearly Master Quality Control Plan should be done as follows:

- The 1st field shall be a capitol letter M.  This denotes the quality control plan as a materials document.

- The 2nd field shall be the district number. (ie…01 for District One, 02 for District Two, etc thru 10 for District Ten)

- The 3rd field is an Alphabet Letter

- The last field will start at 0001 and increase by 1 for each document.

Example --- M03A0001

M = Materials

03 =   District 3

Alphabet Letter   A, B, C, etc.

0001 = last four digits that will increase by one.( 0001, 0002, 0003, Etc.)

# ASPHALT CONCRETE FOR MAINTENANCE

## The provisions of this procedure will also apply to asphalt concrete that is picked up at the plant by the Division's Maintenance forces and Laydown HMA Purchase Orders awarded to contractors. Exceptions to this are as specified in the Purchase Order.

# PROJECT QUALITY CONTROL PLAN

## The Contractor shall submit a letter requesting to use the Master Quality Control Plan for a project.  This letter must be on the Contractor’s letterhead paper and contain the following information:  addressed to the District Engineer/Manager, list the project number, contract identification number, county where the project is located, project description, type of Quality Control Plan and the laboratory reference number for the Master Quality Control Plan. See Attachment #3 for the Plant Letter and Attachment #4 for Feld Letter examples.

## The District shall review the referenced Quality Control Plan to make sure it covers all items in the project.  If the referenced Quality Control Plan is found to be insufficient for some items on the project, the District shall request the Contractor to submit additional information for quality control of those items as an addendum. When the District is satisfied with the Quality Control Plan for this project, an approval letter shall be sent to the Contractor, scanned and attached to contractor’s project Quality Control Plan letter, and then placed in the project’s mail-incoming mailbox in ProjectWise.

### The District approval letter for this project must state the ProjectWise link to the referenced master Quality Control Plan for that Contractor.  Ie…. WVDOT ORGS > District Organization #> Materials > Year>Contractor’s folder > QCP folder > Name of QCP   (ie… 2016 05 21 M08V0007 HMA master field QCP)

6.3	KEY DATES FOR SITE MANAGER

### Once the Quality Control Plan is approved for the project the key date shall be entered in Site Manager by the appropriate District Materials personnel.   The first date entered shall be the date the Project Quality Control Plan letter is received.  The second date shall be when the district approves the quality control plan for use on the project.

____________________________

Ronald L. Stanevich, P.E.

Director

Materials Control, Soils and Testing Division

RLS: Cbe

ATTACHMENTS