WEST VIRGINIA DEPARTMENT OF TRANSPORTATION

DIVISION OF HIGHWAYS

MATERIALS CONTROL, SOILS & TESTING DIVISION

MATERIALS PROCEDURE

ACCEPTANCE CRITERIA FOR EPOXY COATED REINFORCING STEEL

# SCOPE

## To establish a procedure to qualify approved and non-approved coating manufactures of epoxy coated reinforcement steel bars for use on West Virginia Division of Highways (WVDOH) projects.

## To establish a procedure for maintaining a record of such information.

## To establish a procedure for transmitting such information to the districts and to contractors of WVDOH projects.

## This procedure shall apply to epoxy coated steel furnished to West Virginia Division of Highways (WVDOH) projects and purchase orders. The Division may elect to use other control procedures when special conditions dictate.

# APPLICABLE DOCUMENTS

## AASHTO M31 Standard Specification for Deformed and Plain Carbon and Low-Alloy Steel Bars for Concrete Reinforcement, most recent edition.

## ASTM A775 Standard Specification for Epoxy-Coated Steel Reinforcing Bars, most recent edition.

## AASHTO MP18 Standard Specifications for Uncoated, Corrosion-Resistant, Deformed and Plain Chromium Alloyed, Billet-Steel Bars for Concrete Reinforcement and Dowel, most recent edition.

# ACCEPTANCE PROCEDURE

## With each shipment, the coating manufacture shall provide shipping documents which contain either the  coating manufacture’s "Approved Source" number or the approval number that was assigned to the material as per Section 6.

# ACCEPTANCE PROCEDURE FOR APPROVED SOURCE

## For a manufacture to be considered as a source of epoxy coated reinforcing steel bars, the manufacture must submit a certification statement indicating their intention to be included on the WVDOH approved source list as an approved source of epoxy coated reinforcing steel.

## The prospective source shall submit a certified statement that all material shipped to   Division projects will conform to WVDOH specifications. This certified statement shall be signed by a representative of the coating manufacture who has the authority to bind the company.

## The prospective source shall have an acceptable historical record of compliance with WVDOH Specifications.

## All plain steel reinforcement to be coated shall be selected from an approved source list of plain reinforcement steel maintained by the WVDOH

## All epoxy powders used shall be selected from an approved source list of epoxy powders maintained by the WVDOH.

## A copy of the coating manufacture’s Concrete Reinforcing Steel Institute (CRSI) certificate must be submitted indicating conformance to CRSI specifications.

## Samples of epoxy coated reinforcement steel shall be obtained by WVDOH department authorized personnel and shall have the epoxy component tested to ASTM A775 in WVDOH laboratories, unless other methods of verification such as material certifications are used should unforeseen circumstances arise.

## An inspection of the coating facility may be conducted at any time to reinforce confidence in the ability of the facility to produce a quality product.

## Once the above requirements are met, a laboratory approval number will be assigned to the coating facility to indicate WVDOH requirement conformance.  This approval number shall be active for up to two years.  Acceptance of a coaters facility can be verified by accessing the WVDOH online approved source lists.

## Revocation of approved source status may result from revocation or expiration of CRSI Certification or furnishing material that does not comply with Specifications.

# ACCEPTANCE PROCEDURE FOR NON APPROVED SOURCE

## Epoxy coated steel bars that have been coated by a non- approved coating manufacture shall require evaluation on a lot by lot basis under direct coverage provided the material meets the following requirements.

## A copy of the coating manufacture’s CRSI certificate must be submitted indicating current conformance to CRSI specifications.

## Samples of epoxy coated reinforcement steel shall be obtained by WVDOH department authorized personnel to be tested in WVDOH laboratories, unless other methods of verification such as material certifications are used.

## The metallic component of epoxy coated steel bars shall be tested to conform to the requirements of AASHTO M31 or AASHTO MP18.

## The epoxy component of epoxy coated steel bars shall be tested to conform to the requirement s of ASTM A775.

## If the results of the testing reveal that the material is in full compliance with Specifications, an approval number will be issued by the Division that shall be affixed to the shipping documents.

# DOCUMENTATION REPORT

## An updated list of approved epoxy coated reinforcing steel once a year, but no longer than two, and can be updated at any time with a new facility, or with a removal of a facility.

## A current approved list of epoxy coated reinforcing steel shall be available to all contractors, fabricators, and suppliers by accessing the West Virginia Department of Transportation Approved Source.

Ron L. Stanevich, P.E.

Director

Materials Control, Soils and Testing Division

RLS:Prl

http://transportation.wv.gov/highways/mcst/Pages/Listings_Sorted.aspx